## Mirror Mastic: QwikSet™ Mirro-Mastic®

| 1. PRODUCT NAME Mirror Mastic: QwikSet™ Mirro-Mastic® 2. MANUFACTURER Palmer Products Corporation P.O. Box 7155 Louisville, KY 40257 Phone: (800) 431-6151 (502) 893-3668 FAX: (502) 895-9253 Web site: www.mirro-mastic.com E-mail: palmer@mirro-mastic.com |  |
| --- | --- |

3. PRODUCT DESCRIPTION

Basic Use: QwikSet™ is a high quality, fast curing, adhesive mastic formulated for adhering plate glass mirror to various substrates.  Note: Do not use on acrylic mirror or on safety backings.

4. TECHNICAL DATA
Composition and Materials: QwikSet™ is a rubber base adhesive.

Flash point: Less than 0°F,  -18°C TCC

Tensile Strength: 450 psi

Viscosity: 500,000 cps

Color: Black

Application: Caulking gun

Curing Time: 50% strength in 24 hours. 80% strength in 48 hours.  Curing time will depend on temperature, humidity, type of substrate and amount of air that can reach the mastic.

Coverage: With minimum coverage, one cartridge will install approximately 20 square feet (1.9 square meters) of mirror.

Clean up: Mineral spirits

Storage: Ideal storage 50°F to 85°F (10° to 29.4°C)

Shelf life: One year from the date on unopened cartridges.

Packaging: Cartridges (24 cartridges per case)
                    Custom packaging available

WARNING
All Palmer products must be used only for approved purposes, and must be applied only in accordance with Palmer's installation instructions, as set forth in Palmer's specification sheet and installation guides (available upon request from Palmer or its distributors). The user bears all risk of damage, injury or other loss arising out of any non-approved use and/or improper installation of any Palmer product. If Palmer's installation instructions are not followed, in whole or part, for whatever reason, then mechanical fasteners of sufficient size and strength must immediately be used to insure safety of the installation pending prompt proper reinstallation by the product user. Any failure to properly utilize or apply any Palmer product may result in property damage, bodily injury or death. Palmer shall not be responsible for these or any other types of misuse of its products.