BULLET RESISTANT FIBERGLASS

PART 1 GENERAL

1.1  REFERENCE

The publication below forms a part of this specification.

UNDERWRITERS LABORATORY UL 752  9th Edition

Standard for Bullet Resisting Equipment dated Jan. 27,1995

1.2  SUBMITTALS

The following shall be submitted in accordance with Sections 01340 and the SPECIAL CONTRACT REQUIREMENTS: Submit for approval prior to fabrication catalog cuts, brochures, specifications, UL LISTING VERIFICATION, proof of possession of PRODUCT LIABILITY INSURANCE in an amount not less than five million U.S. dollars, and printed data in sufficient detail to indicate compliance with the contract documents and the manufacturer's instructions for the installation of Bullet Resistant Fiberglass.

1.3  DESIGN

Through the design, manufacturing technique and material application the Bullet Resistant Fiberglass shall be of the "non-ricochet type".  This design is intended to permit the encapture and retention of an attacking projectile lessening the potential of a random injury or lateral penetration.

1.4  DELIVERY, STORAGE AND HANDLING

Deliver the materials to the project with the manufacturer’s UL Labels intact and legible.  Handle the material with care to prevent damage.  Store the materials inside under cover, stack flat and off the floor.

1.5  WARRANTY

All materials and workmanship shall be warranted against defects for a period of one (1) year from the date of receipt at the project site.

PART 2 PRODUCTS

2.1  BULLET RESISTANT FIBERGLASS MATERIAL

The panels shall be made of multiple layers of starch-oil woven roving ballistic grade fiberglass cloth impregnated with a thermoset polyester resin and compressed into flat rigid sheets.  The production technique and materials used shall provide the controlled internal delamination to permit the encapture of a penetrating projectile.

BULLET RESISTANT FIBERGLASS  cont.

Bullet Resistant Fiberglass panels shall be UL Listed (BRF100/BRF200/BRF300) manufactured/distributed by:

C.R. Laurence Co., Inc.

2503 E. Vernon Ave.

Los Angeles, CA 90058

Attn: Tech Sales

800-421-6144 Phone

Extension 7760

800-458-7496 Fax

crlaurence.com

Unlisted UL752 bullet resistant fiberglass products will not be considered acceptable or equal.

  - SECURITY LEVEL

The Bullet Resistant Fiberglass must be UL LISTED RATED FOR LEVEL (3/2/1)

  - SUBSTITUTIONS

Other UL Listed bullet resistant fiberglass products are acceptable if in compliance with all requirements of this specification.  Alternate products must be submitted to the architect for approval.

PART 3 EXECUTION

3.1  SUPPORTING MEMBERS

Prior to installing the bullet resistive material the contractor shall verify that all supports have been installed as required by the contract documents and the architectural drawings.

3.2  JOINTS

All joints shall be reinforced by a back-up layer of bullet resistive material.  The bullet resistance of the joint, as reinforced, shall be at least equal to that of the panel.  Minimum width of reinforcing layer at joint shall be 4".  (2" on each panel side or a 2" minimum overlap per side)

3.3  APPLICATION

Armor shall be installed in accordance with the manufacturer's printed recommendations.  Armor panels shall be adhered using an industrial adhesive, mastic, screws or bolts.  Method of application shall maintain the bullet resistive rating at junctures with the concrete floor slab, the concrete roof slab, the bullet resistive door frames, the bullet resistive window frames, and all required penetrations.

** End of Section **