INTERIOR ALUMINUM BULLET RESISTANT

SLIDING TRANSACTION WINDOW

SECTION 08580

# PART 1 – GENERAL

1.01 SUMMARY

- This section includes:

- Interior aluminum bullet resistant sliding transaction windows as indicated in drawings and in sections.

- The publication below forms a part of this specification:

1. UNDERWRITERS LABORATORY UL 752 9th Edition

Standard for Bullet Resisting Equipment dated Jan. 27, 1995.

1.02 SUBMITTALS

- Product Data: Submit Manufacturer’s technical product data substantiating that product complies.

- Shop drawings: Submit for fabrication and installation of windows. Include details, elevations and installation requirement of finish hardware and cleaning.

C.	Certification: Provide printed data in sufficient detail to indicate compliance with the contract documents.

1.03 DELIVERY, STORAGE, AND HANDLING

- Deliver windows crated to provide protection during transit and job storage

- Inspect windows upon delivery for damage. Unless minor defects can be made to meet the Architect’s specifications and satisfaction, damaged parts should be removed and replaced.

- Store windows at building site under cover in dry location.

1.04 PROJECT CONDITIONS

- Field measurements: Check opening by accurate field measurement before fabrication. Show recorded measurements on shop drawings. Coordinate fabrication schedule with construction progress to avoid delay of work.

1.05 WARRANTY

All material and workmanship shall be warranted against defects for a period of one (1)

year from the original date of purchase.

INTERIOR ALUMINUM BULLET RESISTANT

SLIDING TRANSACTION WINDOW

# SECTION 08580 -2

# PART 2 - PRODUCTS

2.01 ACCEPTABLE MANUFACTURER’S

- Basis of design: Design is based on interior aluminum bullet resistant sliding transaction windows, manufactured by C.R. Laurence Co., Inc. (800) 421-6144

Part #s SBRWA1 SBRWA3 SBRWDU1 SBRWDU3 SBRWP1 SBRWP3 SBRWK1 SBRWK3

2.02 MATERIALS

- Frames: 4" Aluminum bullet resistant frame modules shall be to the standards established by U.L. 752 Protection Level _____(specify level 1 or 3).  Frames are to be constructed of 6063-T5 extruded aluminum lined with U.L. listed bullet resistant fiberglass for level 3. Shapes and sizes are to be in accordance with the contract drawings..

- Finish: All aluminum to be clear anodized (A), duranodic bronze (DU), powder (P) or Kynar (K) painted (specify color).

- Glazing: The glazing must be in accordance with U.L. 752 testing standards

Level ____ (specify level 1 or 3).  For level 1 specify 1-1/4" acrylic (with or without SAR abrasion resistant coating). For level 3 specify 1-1/4" laminated polycarbonate with abrasion resistant coating.

D. Options: Keyed lock, burglar bar, counter mounted security clip, full bottom track, half bottom track (no track under sliding panel), shelf/tray, and voice transmission.

1) Shelf: Provide a shelf not less than 2” thick. The shelf is to be the full width of the window and a minimum of 12” deep centered under the glazing. (Shelf Options include: 18” deep shelf, 16 ga. stainless steel #4 finish with or without integral ricochet resistant deal tray, or high pressure laminate shelf, with stainless steel drop-in ricochet resistant deal tray.

2) Voice Transmission: Communication permitted by one of the following as selected by architect: Clear polished 10" disc of same glazing material, held in place in sliding panel over 6" hole with stainless steel standoffs (CAD101 or CAD103) or counter-top electronic thru glass communicator # TTU3 or TTU3J, with or without optional headset.)

PART 3 – EXECUTION

3.01 INSTALLATION

- Install frames and glazing in accordance with manufacturer’s printed instructions and recommendations. Repair damaged units as directed (if approved by the manufacturer and the architect) or replace with new units.

ALUMINUM BULLET RESISTANT TRANSACTION WINDOW

SECTION 08580 -3

3.02 CLEANING

A.	Clean frame and glazing surfaces after installation, complying with requirements contained in the manufacturer’s instructions. Remove excess glazing sealant compounds, dirt or other substances.

3.03 PROTECTION

A.	Institute protective measures required throughout the remainder of the construction period to ensure that all the windows do not incur any damage or deterioration, other than normal weathering, at the time of acceptance.

## END OF SECTION